AN INVESTIGATION OF NANO-PHASE GOETHITE AND ITS ROLE IN PROTECTIVE RUST FORMATION

by

Jonathan Wood

A Senior Thesis submitted to the Faculty of the Department of Physics Old Dominion University in Partial Fulfillment of the Requirement for the Degree of

BACHELOR OF SCIENCE

OLD DOMINION UNIVERSITY

MAY 2005

Approved by:

______________________________

Dr. Desmond C. Cook (Advisor)

______________________________

Dr. Gary Copeland

______________________________

Dr. Charles I. Sukenik

ABSTRACT

AN INVESTIGATION OF NANO-PHASE GOETHITE AND ITS ROLE IN PROTECTIVE RUST FORMATION

# Jonathan Wood

Old Dominion University, April 2005

Advisor: Dr. Desmond C. Cook

Recent research in corrosion science has revealed that goethite (-FeOOH) is an important iron oxide in the formation of protective, adherent rust layers on exposed steel.  Moreover, these adherent properties seem to be attributed to small particle, nano-phase goethite.  The investigation of goethite includes particles ranging in sizes between 10-200nm, both pure and chromium substituted, using Mössbauer spectroscopy at 300K, 77K, and 4K.  The analysis of these spectra produced a reliable means of quickly identifying particle size and magnetic properties.  A 15nm particle at 300K has an average hyperfine interaction of 13.28T while a 50nm particle has an average interaction of 35.10T.  Similarly, differences between chromium substituted and pure goethite were found using Mössbauer spectroscopy. A 15nm pure particle at 4K has an average hyperfine interaction of 49.69T while a 15nm Chromium substituted particle as an interaction of 49.84T.

Acknowledgments

I would like to express my gratitude to Dr. Cook for being my mentor and providing me important insight into the corrosion process throughout the entire project.

I would also like to thank Old Dominion University for providing funding through the Undergraduate Research Program (2005) to make this research possible.

Table of Contents

Page

1.	Introduction	1

1.1	Types of Steel	1

1.2	Research Motivation	2

1.3	Current and Past Research	3

2.	Sample and Analytical Techniques	8

2.1	Samples	8

2.2	X-ray Diffraction	9

2.3	Mössbauer Spectroscopy	13

2.3.1	Isomer Shift	14

2.3.2	Electric Quadrupole Interaction	15

2.3.3	Magnetic Zeeman Effect	16

2.3.4	Laboratory Equipment	16

2.3.5	Methodology	19

2.3.6	Magnetic Relaxation	19

3.	Results		21

3.1	Pure Goethite Mössbauer Data	21

3.2	Chromium Substituted Mössbauer Data	22

3.3	4K Analysis of Pure and Chromium Substituted Goethite	31

4.	Conclusion	33

4.1	Research Findings	33

4.2	Future Research	33

5.	Bibliography	34

Table of Figures and Tables

Page

Figure 1(a): EPMA Photograph of a cross section of exposed steel	5

Figure 1(b): EPMA Cross-section from exposed steel sample	5

Figure 2: TEM Photographs of Cr substituted samples	6

Figure 3: Particle size vs Cr concentration for YAM samples	10

Figure 4: XRD spectra of Al2O3	11

Figure 5: XRD spectra of common iron oxides	12

Figure 6: Illustration of Mössbauer splitting in Fe	17

Figure 7: Mössbauer instrumentation	18

Figure 8: Overlay of Mössbauer spectra of goethite at 300K and 77K	20

Figure 9(a): Comparison of pure goethite magnetic field at 300K and 77K	21

Figure 9(b): Comparison of pure goethite magnetic field at 77K	22

Figure 10(a): Comparison of Cr goethite magnetic field at 300K and 77K	23

Figure 10(b): Comparison of Cr goethite magnetic field at 77K	23

Figure 11: Cr goethite Mössbauer spectra at 300K	24

Figure 12: Pure goethite Mössbauer spectra at 300K	25

Figure 13: Cr goethite Mössbauer spectra at 77K	26

Figure 14: Pure goethite Mössbauer spectra at 77K	27

Figure 15: Cr goethite Mössbauer spectra at 4K	28

Figure 16: Pure goethite Mössbauer spectra at 4K	29

Figure 17: Magnetic field distribution at 300K	30

Figure 18: Magnetic field distribution at 77K	30

Figure 19: Overlay of Mössbauer spectra in 15nm Cr and pure	31

Figure 20: Comparison of magnetic fields in Cr and pure goethite at 4K	32

Table 1: Common iron oxides	3

Table 2: Goethite sample dimensions	8